Split singularities and dislocation injection in strained silicon

Martijn Feron1,2, Zhen Zhang1 and  Zhigang Suo1,a

1 School of Engineering and Applied Sciences, Harvard University, Cambridge, MA 02138, USA

2 Faculty of Mechanical Engineering, Technische Universiteit Eindhoven, 5600 MB, The Netherlands

Abstract:

The mobility of charge carriers in silicon can be significantly increased when silicon is subject to a field of strain.  In a microelectronic device, however, the strain field may be intensified at a sharp feature, such as an edge or a corner, injecting dislocations into silicon and ultimately failing the device.  The strain field at an edge is singular, and is often a linear superposition of two modes of different exponents. We characterize the relative contribution of the two modes by a mode angle, and determine the critical slip systems as the amplitude of the load increases.  We calculate the critical residual stress in a thin-film stripe bonded on a silicon substrate.

a)  email:  suo@deas.harvard.edu

I. Introduction

In microelectronic devices, strains are deliberately introduced into silicon to increase the mobility of electrons or holes; see Ref. [1] for a review.  The strains, however, may cause mechanical failure.  In particular, the devices usually contain sharp features like edges and corners, which may intensify strains and emit dislocations into silicon, failing the devices. 2,3   We recently described a method to predict conditions under which such sharp features do not emit dislocations.4  The method is further developed in the present paper to account for split singularities. 5,6

Fig. 1 illustrates the structure to be studied.  A blanket film, of thickness h and residual stress σ, is grown on the (001) surface of a single-crystal silicon substrate.  The film is then patterned into a stripe of width L, with the side surfaces parallel to the (110) plane of silicon.  When the film covers the entire surface of the substrate, the film is in a state of uniform stress, and the substrate is stress-free.  When the film is patterned into a stripe, a field of stress builds up in the substrate, and concentrates at the root of each edge. It is this concentrated stress that injects dislocations into silicon.

The structure in Fig.1 is similar to those studied in Refs. [4, 7-12], but this paper will examine a specific aspect:  split singularities.  It is well known that, at the tip of a crack in a homogeneous elastic material, under the plane strain conditions, the singular stress field is a linear superposition of two modes, the tensile mode and the shearing mode, both modes having the exponent of ½.  More generally, at the tip of bonded wedges of dissimilar materials, the singular stress field may still consist of two modes, but usually of unequal exponents, either a pair of complex conjugates, or two unequal real numbers.6,13-16  The case of complex-conjugate exponents has been extensively discussed within the context of a crack lying on a bimaterial interface. 17  The present paper will focus on the case that the two modes have unequal real exponents.  That is, a stronger and a weaker singularity coexist.  It has been shown that both singularities can be important in causing failure. 5,6,16   Section II will describe the linear superposition of two modes of singular stress fields.  Section III will investigate which slip systems will be activated.  Section IV will calculate the critical residual stress in the thin-film stripe for injecting dislocations into the silicon substrate.

II. A linear superposition of two modes of singular stress fields

The inset of Fig.2 illustrates an edge of the thin film bonded on the substrate, along with a system of polar coordinates r,θ,z.  In this view focused on the root of the edge, the film takes the quarter space, 00≤θ≤900, and the substrate takes the half space, −1800≤θ≤00.  The two materials are bonded along the interface, θ=00.  Both materials are taken to be elastic and isotropic.  For problems of this type Dundurs18 showed that the stress field depends on elastic constants through two dimensionless parameters:

α=μf1−νs−μs1−νfμf1−νs+μs1−νf.	(1)

β=12μf1−2νs−μs1−2νfμf1−νs+μs1−νf.	(2)

where μ is the shear modulus, and ν Poisson’s ratio.  The subscripts f and s refer to the film and the silicon substrate, respectively.  By requiring 0≤ν≤0.5 and μ>0, the Dundurs parameters are confined within a parallelogram in the α,β plane, with vertices at 1, 0, 1, 0.5, −1, 0 and −1, −0.5.

For a singular field around the root of the edge, each component of the stress tensor, say σθθ, takes the form of σθθ~r−λ.  This singular stress field is determined by an eigenvalue problem, resulting in a transcendental equation that determines the exponent λ. 19,20,21  The exponent is restricted as 0<Reλ<1, a restriction commonly adopted, with justifications critiqued in Refs. [22,23].  For the specific geometry illustrated in the inset, Fig. 2 plots the contours of the exponents on the α,β plane.  The parallelogram is divided into two regions by a dark curve.  In the lower-left region, the exponents are two unequal real numbers, one stronger (λ1) and the other weaker (λ2). The values for λ1 are labeled horizontally, and those for λ2 are labeled vertically.  In the whole region, λ2<λ1≤0.5.  In the upper-right region, the exponents are a pair of complex conjugates, λ1,2=ξ±iε. The real part is depicted by solid lines and labeled horizontally, while the imaginary part is depicted by dashed lines and labeled vertically.  At each point on the boundary (i.e., the dark curve), the two exponents degenerate to one number:  when the point is approached from a region of real exponents, the two real exponents become identical; when the point is approached from a region of complex-conjugate exponents, the imaginary part vanishes.  When α=1, i.e, the film is rigid, the singularity exponents are the same as those for an interfacial crack, λ1,2=0.5±iε, with ε=1(2π)ln1−β1+β. 24

As noted in Ref. [5], when the two materials have similar elastic constants, i.e., when α=β=0, the two modes of singular fields can be interpreted readily.  In this case, the line bisecting the angle of the wedge is a line of symmetry.  The stronger mode corresponds to a stress field symmetric about this line (i.e., the tensile mode).  The weaker mode corresponds to a stress field anti-symmetric about this line (i.e., the shearing mode).  When the two materials have dissimilar elastic constants, however, the symmetry is broken, and the two modes may not be interpreted in such a simple way.

Following a common practice, in this paper we will use α to represent the elastic mismatch, and neglect the effect of β by setting β=0.  When β=0, the exponents are two unequal real numbers, regardless the values of α.

We next paraphrase several fundamental ideas in fracture mechanics.25  Once we retain the two unequal exponents, the stress field around the root of the edge is a linear superposition of the two modes:

σijr,θ=k12πrλ1Σij1θ+k22πrλ2Σij2θ.	(3)

The angular functions Σij1θ and Σij2θ are normalized such that Σrθ10=Σrθ20=1, and their full expressions are listed in Appendix A.  The stress intensity factors, k1 and k2, are determined by the external boundary conditions, as described in Section IV.

The singular stress field (3) is obtained by assuming that the materials are elastic, and the edge is perfectly sharp.  Such assumptions are invalid in a process zone around the root of the edge.  Let Λ be the size of the process zone, within which the singular stress field (3) is invalid.  Also, the singular stress field (3) is invalid at size scale h, where the external boundary conditions will change the stress distribution.  However, provided the process zone is significantly smaller than the macroscopic length, Λ<<h, the singular stress field (3) prevails within an annulus, known as the k-annulus, of some radii bounded between Λ and h.

The two parameters, k1 andk2, have different dimensions, stresslengthλ1 and stresslengthλ2, respectively.  We introduce a convention by writing

k1=SΛλ1cosψ,      k2=SΛλ2sinψ.	(4)

This convention is illustrated in Fig. 3.  Here S and ψ characterizes the stress field at length scale Λ, with S characterizing the amplitude of the stress field, and ψ characterizing the relative contribution of the two modes.  Since both k1 and k2 can be either positive or negative, the mode angle can be in the entire range of 0≤ψ<3600.

The microscopic process of dislocation emission occurs within the process zone, but is driven by the stress field (3) in the k-annulus. Dislocations emit from the root when the amplitude S  reaches a critical value Sc, namely,

Sψ=Scψ.  	(5)

The amplitude S and the mode angle ψ are determined by the external boundary conditions, by solving a boundary value problem of linear elasticity.  The critical condition Scψ is determined either by experimental measurement or by computation from a microscopic model of the emission process.

III. Selection of critical slip system

Table I lists the twelve slip systems in silicon.  Given a mode angle, ψ, as the amplitude S increases, some slip systems will activate earlier than others.  We select the critical slip systems by the following procedure.  For each slip system, we use the stress field (3) to calculate the resolved shear stress at distance r=Λ.  The slip system with the maximum resultant shear stress is taken to be the critical slip system.

For a given slip system, let ni be the unit vector normal to the slip plane, and bj be the Burgers vector.  Under a general state of stress σij, the resolved shear stress on the slip system is

τnb=σijnibjb.	(6)

A combination of (3), (4) and (6) gives the resolved shear stress at the distance r=Λ by

τnbS=cosψΣij1θnibj2πλ1b+sinψΣij2θnibj2πλ2b.	(7)

Because this procedure only invokes the magnitude, not the direction, of the resolved shear stress, a simultaneous change in the sign of the two stress intensity factors k1 and k2 will not change the condition of dislocation emission.  Consequently, we can restrict the range of the mode angle to −900≤ψ≤900.  Indeed, the right-hand side of (7) is a function of ψ with a period of 1800.

An inspection of Fig. 1 shows that the slip systems 12111110 and 12111110 are of zero resolved shear stress.  The slip systems 1211110 {1 and 1211101 {1 are of identical resolved shear stress and with fixed polar angle θ=−125.260. Other similar pairs of slip systems are listed in Table I.  By contrast, the resolved shear stress for slip systems 12111110 and 12111110 is a function of polar angle θ.  As an example, in Fig. 4(a), the resolved shear stress is plotted as a function of θ for ψ=0 and α=0.5.  The polar angle θ corresponding to the maximum resolved shear stress is selected as the critical angle where the potential dislocation is nucleated.  In Fig. 4(b), the critical polar angle θ in the loading range −900≤ψ≤900 is plotted for α=0.5.  This procedure can be repeated for all values of α.

For α=0.5, Fig. 5 (a) plots the resolved shear stresses as a function of the mode angle ψ for all twelve slip systems.  The slip system with largest resolved shear stress is the potential slip system on which dislocations are firstly injected.  The slip systems so selected are marked as the critical slip system for the whole range value of −900≤ψ≤900.  Obviously, different slip systems can be activated for different values of mode angle ψ.  Similarly, the critical slip systems for any material combination under any mode angle can be selected, such as shown in Fig. 5(b) for α=0 and in Fig. 5(c) for α=−0.5.

IV.  The critical condition for dislocation emission

The stress field around the root of the edge is described by Eq.(3). Linearity and dimensional consideration dictate that the stress intensity factors k1 and k2 should take the form

k1=σhλ1f1Lh,α,k2=σhλ2f2Lh,α	(8)

where the dimensionless functions f1Lh,α and f2Lh,α are determined as follows.  We calculate the full stress field in the structure by using the finite element package ABAQUS, then fit the interfacial shear stress close to the root, say 10−3<rh<10−2, to the equation

σrθθ=0=k12πrλ1+k22πrλ2, 	(9)

with k1 and k2 as fitting parameters.  The two functions so calculated are plotted in Fig. 6.  The trend is understood as follows.  Although the stress field intensifies at the root, the side surface of the stripe is traction-free.  When the stripe is very narrow, Lh→0, the stress in the stripe is almost fully relaxed.  When the stripe is very wide, Lh→∞, the stress field near one edge of the stripe no longer feels the presence of the other edge, so f1 and f2 attain plateaus.

A combination of (4) and (8) gives the mode angle ψ as

tanψ=f2f1Λhλ1−λ2	(10)

Take the typical value of film thickness h=100nm, and take the process zone size Λ to be the Burgers vector in silicon b=0.383nm.  Figure 7 plots the mode angle ψ as a function of the Dundurs parameter α for aspect ratio of the stripe, Lh=2 and 20.  We observe that for the values of α<0, i.e. when the film is more compliant than the substrate, both the elastic mismatch and the aspect ratio have negligible effects on the mode angle ψ, and the weaker singular term in Eq.(3) is negligible, so that the singular stress field (3) can be simplified to the single mode.  However, for positive values of α, i.e., when the film is stiffer than the substrate, the mode angle ψ increases very fast, and both singular terms in (3) should be taken into account.

We now comment on the case studied in Ref. [4].  The film stripe is SiN with shear modulus 54.3GPa and Poisson’s ratio 0.27.  The silicon substrate is of shear modulus 68.1GPa and Poisson’s ratio 0.22.  The elastic mismatch is small, α≈0. The singularity exponents areλ1=0.4514 and λ2=0.0752.  Still taking h=100nm and b=0.383nm, we obtain that ψ=0.20 for Lh=20, and ψ=1.270 for Lh=2.  Evidently in this case the weaker singularity makes negligible contribution.  From Fig. 5(b), we identify the critical slip systems are 1211101 {1 and 1211110 {1, which is predicted in Ref. [4].

We now calculate the critical residual stress in the thin-film stripe to inject dislocations into silicon.  We assume that the critical condition is reached when the the maximum resolved shear stress reaches the theoretical shear strength at distance r=b.  The theoretical shear strength is estimated by τth=0.2μ, where μ is the shear modulus of silicon.26   Setting τnbb=τth, a combination of Eqs. (3), (6) and (8) gives a scaling relation between the critical residual stress and the feature sizes:

σcμ=0.2hbλ1Σij1θ2πλ1f1+hbλ2Σij2θ2πλ2f2nibjb−1.	(11)

Figures 5 and 7 show that the critical slip systems are 1211101 {1 and 1211110 {1.  We plot in Fig. 8  the normalized critical stresses as a function of the aspect ratio L/h for Dundurs α=0.5, 0, -0.5.  A plateau is reached for large values of the aspect ratio L/h. When the aspect ratio is decreased, the critical stress will drastically improve, implying the fact that a narrow stripe might not inject dislocations into the silicon substrate, while a wide stripe could inject dislocations.  Also evident is that the critical stress increases as the film becomes stiffer.  This is because the same level of residual stress in a stiff film will induce a low level of stress if the substrate is relatively compliant.

V. Concluding remarks

The singular stress field at a root of an edge is a linear superposition of two modes, with different exponents.  A mode angle ψ is introduced to measure the relative contribution of the two modes to the failure conditions.  Figure 2 shows that the two exponents are very different when the film is compliant relative to silicon, and are very similar when the film is stiff relative to silicon.  Consequently, as shown in Fig. 7, the weaker singular field is negligible when the film is compliant, but is significant when the film is stiff.  For the full range of the mode angle, we describe a procedure to select the critical slip systems.  On the basis of the criterion that dislocations nucleate when the resolved shear stress at distance b from the root of the thin-film edge reaches the theoretical strength, we calculate the critical residual stress in the stripe, and show that the critical stress is low when the stripe is wide or compliant.

Acknowledgement.  This work is carried out when the authors are supported by Intel Corporation through a contract via the Semiconductor Research Corporation (award number 2005-KJ-1369), and by the National Science Foundation through the MRSEC at Harvard University.

References

- M. Ieong, B Doris, J. Kedzierski, K. Rim, and M. Yang, Science 306, 2057 (2004).

- M. Dellith, G.R. Booker, B.O. Kolbesen, W. Bergholz, and F. Gelsdorf, J. Electrochem. Soc. 143, 210 (1996).

- M. Miyake and M. Takahashi, J. Electrochem. Soc. 144, 1020 (1997).

- Z. Zhang, J. Yoon, and Zhigang Suo, Appl. Phys. Lett. 89, 261912 (2006).

- X. H. Liu, Z. Suo, and Q. Ma, Acta Mater. 47(1), 67 (1999).

- Z. Zhang and Z. Suo, Int. J. Solids Struct. (2006) http://dx.doi.org/10.1016/j.ijsolstr.2006.11.035

- M. Kammler, D. Chidambarrao, K.W. Schwarz, C.T. Black, and F.M. Ross, Appl. Phys. Lett. 87, 133116 (2005).

- S. M. Hu, Appl. Phys. Lett. 32, 5 (1978); J. Appl. Phys. 50, 4661 (1979); 70, R53 (1991).

- S.C. Jain, H.E. Maes, K. Pinardi, and I. De Wolf, J. Appl. Phys. 79, 8145 (1996).

- S. Isomae, J. Appl. Phys. 52, 2782 (1981).

- J. Vanhellemont, S. Amelinckx and C. Claeys, J. Appl. Phys. 61, 2170 (1987); 61, 2176 (1987); 63, 5703 (1988).

- K.W. Schwarz and D. Chidambarrao, J. Appl. Phys. 85, 7198 (1999).

- A.R. Akisanya and N.A. Fleck, Int. J. Solids Structures 34, 1645 (1997).

- I. Mohammed And K.M. Liechti, J. Mech. Phys. Solids 48, 735 (2000).

- E.D. Reedy, Int. J. Solids Struct. 37, 2429 (2000).

- P.E.W. Labossiere, M.L. Dunn, and S.J. Cunningham, J. Mech. Phys. Solids 50, 405 (2002).

- J.R. Rice, J. Appl. Mech. 55, 98 (1988).

- J. Dundurs, J. Appl. Mech. 36, 650-652 (1969).

- M.L. Williams, J. Appl. Mech. 19(4), 526 (1952).

- D. B. Bogy, J. Appl. Mech. 38, 377 (1971).

- J.R.Barber, Elasticity, 2nd ed., (Kluwer, Dordrecht, 2002).

- C.Y. Hui and A. Ruina, Int. J. Fracture 72, 97 (1995).

- M.L. Dunn, C.Y. Hui, P.E.W. Labossiere and Y.Y. Lin, Int. J. Fract. 110, 101 (2001).

- N. Lu and Z. Suo,  2007 (unpublished).

- B. Lawn, Fracture of Brittle Solids, 2nd ed., (Cambridge University Press, 1993).

- J. P. Hirth and J. Lothe, Theory of dislocation, 2nd ed. (Krieger Publishing Company, Malabar, Florida, 1992), p. 6.

### Appendix A.  Stress components in polar coordinates and crystal coordinates

The singular stress field Eq.(3) is solved by the methods outlined in Ref. [10, 5]  The eigenfunctions Σijθ associated with the eigenvalue λ are expressed in polar coordinates r,θ,z as

Σrrθ=−λ−1λ−2Asinλ−2θ+Bcosλ−2θ+λ+2Csinλθ+Dcosλθ,	(A.1)

Σθθθ=λ−1λ−2Asinλ−2θ+Bcosλ−2θ+Csinλθ+Dcosλθ, 	(A.2)

Σrθθ=λ−1λ−2Acosλ−2θ−Bsinλ−2θ+λCcosλθ−Dsinλθ,	(A.3)

Σzzθ=−4νλ−1Csinλθ+Dcosλθ, 		(A.4)

Σrz=Σθz=0.		(A.5)

The eigenvalue λ and its associated coefficients A, B, C and D in the film and the substrate are solved by the boundary conditions.  In this paper, the singular stress field in the silicon substrate around the root of the edge causes dislocation to be emitted, so that the eigenvalues and the associated coefficients only in the substrate are listed in Table II (for α=0.5, 0, -0.5 with β=0).

In calculating the resolved shear stress Eq.(6), the stress components in the crystal coordinates x1,x2,x3, σij, are converted from those in the polar coordinates r,θ,z. The relation of x1,x2,x3 and r,θ,z is depicted in Fig.1, and the matrix of conversion is

Q=−cosθ/2−cosθ/2sinθsinθ/2sinθ/2cosθ−1/21/20	(A.6)

From σcrystal=QTσpolarQ, the stress components in crystal coordinates are

σ11=σ22=σrrcos2θ+σθθsin2θ+σzz−σrθsin2θ2	(A.7)

σ12=σ21=σrrcos2θ+σθθsin2θ−σzz−σrθsin2θ2	(A.8)

σ13=σ31=σ23=σ32=σθθ−σrrsin2θ−2σrθcos2θ22	(A.9)

σ33=σrrsin2θ+σθθcos2θ+σrθsin2θ		(A.10)

Table I. The twelve slip systems and the corresponding critical polar angles are listed.

| Slip plane, n | Slip direction, b | Critical polar angle, θ* |
| --- | --- | --- |
| (111) | [110] | −125.26∘ |
|  | [101] | −125.26∘ |
|  | [011] | −125.26∘ |
| (111) | [110] | *Fig. 4 |
|  | [101] | −125.26∘ |
|  | [011] | −54.74∘ |
| (111) | [110] | −54.74∘ |
|  | [011] | −54.74∘ |
|  | [101] | −54.74∘ |
| (111) | [110] | *Fig. 4 |
|  | [101] | −54.74∘ |
|  | [011] | −125.26∘ |

*For slip systems  12111110 and 12111110, the critical polar angle, i.e. the polar angle for which the resolved shear stress has a maximum, depends on the mode angle. This dependence is depicted in Fig 4.

Table II. Singularity exponents and the associated coefficients in Eqs.(A.1)–(A.5) in silicon substrate for α=0.5, 0, -0.5 with β=0.

|  | -0.5 |  | 0 |  | 0.5 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0.4314 | 0.0168 | 0.4555 | 0.0915 | 0.4783 | 0.2542 |
| A | 0.9803 | -0.3775 | 0.9885 | 0.1427 | 0.9951 | 0.4213 |
| B | 0.2687 | -9.6738 | 0.3695 | -1.9826 | 0.4717 | -0.9088 |
| C | -0.5123 | -105.1100 | -0.6804 | -9.0562 | -0.8414 | -2.3815 |
| D | 1.8693 | 4.1015 | 1.8201 | -0.6517 | 1.7750 | -1.1040 |

Fig. 1.  A blanket thin film, of thickness h and residual stressσ, is grown on the (001) surface of a single-crystal silicon substrate.  The film is then patterned into a stripe of width L, with the side surfaces parallel to the (110) plane of silicon.

Fig. 2.  The inset shows the root of an edge of a thin film bonded on a substrate.  Contours of the singular exponents are plotted on the plane of the Dundurs parameters (α,β).  The parallelogram is divided into two regions by a dark curve. In the lower-left region, the exponents are two unequal real numbers, with the larger one labeled horizontally and the smaller one labeled vertically. In the upper-right region, the exponents are a pair of complex conjugates, with real part depicted by solid lines and labeled horizontally, and the imaginary part depicted by dashed line and labeled vertically.

Fig. 3.  The graphical representation of the amplitude S and the mode angle ψ.

(a)

(b)

Fig. 4.  The normalized resolved shear stress for slip systems 12111110 and 12111110 is a function of the polar angle θ.  As an example, in (a), the normalized shear stress is plotted as a function of θ.  The polar angle θ corresponding to maximum resolved shear stress is selected and marked by “” as the critical angle where the potential dislocation is nucleated.  In (b), all the critical polar angle θ in the range −900≤ψ≤900 is plotted for α=0.5.

(a)

(b)

(c)

Fig. 5. Normalized resolved shear stresses are plotted as a function of mode angle for all of the twelve slip systems.  The slip system with largest resolved shear stress is the potential slip system on which the dislocation is firstly injected, so those slip systems are selected and marked for the whole range of the mode angle, −900≤ψ≤900.    (a) α=0.5  (b) α=0  (c) α=−0.5.

Fig. 6	The normalized stress intensity factors, f1 and f2, are plotted as a function of the aspect ratio, Lh, of the stripe on the silicon substrate.

Fig. 7	Mode angle ψ is plotted as a function of Dundurs parameterα for aspect ratio of the stripe, Lh=2 and 20.

Fig. 8	Normalized critical stresses are plotted as a function of the aspect ratio L/h for Dundurs parameter α=0.5, 0, -0.5.