Homework

Due Friday, 12 October

11.  Positive-definite elastic energy density

It is reasonable to require that the elastic energy density be a positive-definite quadratic form of the strain tensor. That is,  for any state of strain, except that  when the strain tensor vanishes. For an isotropic, linearly elastic solid, confirm that this positive-definite requirement is equivalent to require that  and .

12.  The coefficient of thermal expansion (CTE) is a second-rank tensor.

When an anisotropic solid is subject to a change in temperature, all components of the strain tensor can change.  Consequently, the coefficient of thermal expansion (CTE) is a second-rank tensor.  For a crystal of cubic symmetry, show that the CTE is the same in all directions.

13.  Hooke's law for anisotropic, linearly elastic solids

Hooke's law connecting stresses ij and strains ij for a generally anisotropic solid can be written in one of the following forms

The usual correspondence is adopted, i.e.

The fourth-order tensors S and C are the compliance and stiffness tensors, respectively.  The 6by6 matrices s and c (s = c-1) are conventional compliance and stiffness matrices.

i)  Confirm that

ii)  Let m = miei be a unit vector.  Show that when the solid is under a uniaxial stress in the direction m, Young's modulus in this direction is given by

iii)  For a cubic solid show the Young's modulus in direction m is given by

iv)  Find the orientations for a cubic solid which attain minimum or maximum Young's modulus.

14.  Invariants of a tensor

When the basis changes, the components of a vector change, but the length of the vector is invariant.  Let be a vector, and  be the components of the vector for a given basis.  The length of the vector is the square root of

.

The index i is dummy.  Thus, this combination of the components of a vector is a scalar, which is invariant under any change of basis.  For a vector, there is only one independent invariant.  Any other invariant of the vector is a function of the length of the vector.

This observation can be extended to high-order tensors.  By definition, an invariant of a tensor is a scalar formed by a combination of the components of the tensor.  For example, for a symmetric second-rank tensor , we can form three independent invariants:

.

In each case, all indices are dummy, resulting in a scalar.  Any other invariant of the tensor is a function of the above three invariants.

Actions:

- For a nonsymmetric second-rank tensor, give all the independent invariants.  Write each invariant using the summation convention, and then write it explicitly in all its terms.

- Give all the independent invariants of a third-rank tensor.  Use the summation convention.