Homework

Due Friday, 14 December

37. Yield conditions under the biaxial stress states

A metal has the yield strength  under the uniaxial stress state. Load a sheet of this metal into a biaxial stress state,  in the x-direction and  in the y-direction. The two stress components can have different magnitudes, and can be either tensile or compressive. All the other stress components are zero.

- Obtain the yield condition according to the von Mises criterion. Represent the yield condition on the plane spanned by  and .

- For this part of the problem, assume that the uniaxial yield strength is , and the applied loads are such that the two stress components are related as , with being compressive and  being tensile. According to the von Mises criterion, at what stresses  and  will the sheet yield?

38. Design a rotating disk to avert plastic deformation

The problem of the stresses in disks spinning at high speed is of vital importance in the design of many machines. We now model a solid disk in the polar coordinates , and calculate the stresses in the disk caused by the centrifugal force. The nonzero stress components are  and .  Recall the relations between the radial displacement  and the strains:

.

(a)	Apply Newton’s second law to a differential element in the polar coordinates, and show that

,

where  is the angular velocity, and  the density.

(b)	Assume the disk deforms elastically. Formulate a boundary value problem and determine the stress field in the disk.

(c)	If you want to design a steel disk to rotate at 3600 rotations per minute (rpm), what is the largest radius that the disk can have? Take  = 7800 kg/m3, E = 210 GPa,  = 0.3, y = 500 MPa.

(d)	Determine the stress field in the disk as a function of angular velocity in case the velocity is high enough to develop a plastic region in the disk. Assume the material follows a piecewise linear stress-strain law, with modulus E, yield stress y and strain hardening exponent n.

39. A stress history with J2-flow theory

The uniaxial tensile stress-strain curve of an initially isotropic material is given by the following piecewise power-hardening relation:

where o = o/E. Calculate the history of the two plastic strain components given the following history of stress:

(OA) 11 increases to 1.5o with 12 = 0

(AB) 12 increases to o with 11 = 1.5o

Plot the results in the form p11/o versus 12/o and p12/o versus 12/o for the segment AB with n = 3 for J2-flow theory.

40. Another problem on J2-flow theory

An initially isotropic material is stressed into the plastic range by simple tension to a stress level 11 = . Find the coefficients for the subsequent increment of deformation in the equations

according to J2-flow theory. Assume the constitutive relation is fit to the uniaxial stress-strain curve and the tangent modulus and secant modulus at  are Et and Es.