Interfacial Thermal Stresses in a Bi-Material Assembly 
with a Low-Yield-Stress Bonding Layer

E. Suhir, 
University of California, Santa Cruz, CA, 
University of Maryland, College Park, MD,
and ERS Co., 727 Alvina Ct., Los Altos, CA 94024

tel. 650-969-1530, fax. 650-968-4611,  cell. 408-410-0886 suhire@aol.com
Abstract
An approximate predictive model is developed for the evaluation of the interfacial thermal stresses in a soldered bi-material assembly with a low-yield-stress bonding material. This material is considered linearly elastic at the strain level below the yield point and ideally plastic at the higher strains. The results of the analysis can be used for the assessment of the thermally induced stresses in bonding materials in some laser packages and in similar micro- and opto-electronic assemblies.
Introduction

Adhesively bonded and soldered bi-material assemblies are widely used in micro- and opto-electronics [1-16]. Interfacial stresses in such assemblies, when subjected to temperature excursions, concentrate at the peripheral portions of the assembly. Plastic strains occur in the bonding material, if the induced strains exceed the yield point. The low cycle fatigue conditions, when the assembly is subjected to temperature cycling, make such a bonding material vulnerable and thereby responsible for the fatigue strength of the assembly. 
In the analysis that follows we develop an approximate analytical model for the assessment of the interfacial stresses in a bi-material soldered assembly with a low-yield-stress of the bonding material. The developed model is an extension of the models developed previously for the case of an elastic bonding layer [5, 6]. The model can be used in the analysis and design of soldered assemblies with solders that are characterized by a low yield strain. 
The analysis is carried out under a major assumption that the bonding material is linearly elastic at the strain level below the yield strain and is ideally plastic at the levels exceeding the yield strain. It is clear that the previously obtained elastic solution [5, 6], on one hand, and the present ideally-elastic/ideally-plastic solution, on the other, address the two extreme cases. The more general situation, when the bonding material experiences elasto-plastic deformations above the yield point, is beyond the scope of the present analysis.
Analysis

Assumptions
The following major assumptions are used in this analysis:
· The bonded components can be treated, from the standpoint of structural analysis, as elongated rectangular plates that experience linear elastic deformations 

· Approximate methods of structural analysis (strength-of-materials) and materials physics, rather than methods of elasticity and plasticity, can be used to evaluate stresses and displacements (see, for instance, [12])
· At least one of the assembly components (the “substrate”/”submount”) is thick and stiff enough, so that this component and the assembly as a whole do not experience bending deformations. The thinner component, however, might experience some bending with respect to the thicker component (Fig.1)
· The bonding material behaves in a linearly elastic fashion, when the induced shearing strain is lower than the strain that corresponds to the yield point, and in an ideally plastic fashion, when this strain exceeds the yield strain of the bonding material
· The yield stress in shear, 
[image: image1.wmf]Y

t

, if unknown, can be assessed from the yield stress in tension, 
[image: image2.wmf]Y

s

, based on the von-Mises formula (see, for instance, [12])

·                                                             
[image: image3.wmf]Y

t

=
[image: image4.wmf]Y

s

/
[image: image5.wmf]3

                                                           (1)

· The interfacial shearing stresses can be evaluated based on the concept of the interfacial compliance [5,6], without considering the effect of “peeling”, i.e., the normal interfacial stresses acting in the through-thickness direction of the assembly. The “peeling” stress can be then determined from the evaluated interfacial shearing stress

· The “peeling” stress is proportional to the deflections of the thinner component of the assembly, i.e., to its displacements with respect to the thicker component.

Shearing Stress

Basic Equation

Let an elongated soldered bi-material assembly (Fig.1) be manufactured at an elevated temperature and subsequently cooled down to a low (say, room) temperature. In an approximate analysis, the longitudinal interfacial displacements, 
[image: image6.wmf])

(

1

x

u

and 
[image: image7.wmf])

(

2

x

u

, of the adherends (assembly components) can be sought, within the elastic mid-portion, 
[image: image8.wmf]*

*

x

x

x

£

£

-

, of the assembly (
[image: image9.wmf]*

x

±

 are the coordinates of the boundaries of the elastic mid-portion), in the form [5]:

                                       
[image: image10.wmf]),

(

)

(

)

(

),

(

)

(

)

(

0

2

2

2

2

0

1

1

1

1

x

d

T

tx

x

u

x

d

T

tx

x

u

x

x

t

k

x

x

l

a

t

k

x

x

l

a

ò

ò

+

-

D

-

=

-

+

D

-

=

                                    (2)

where  
[image: image11.wmf]1

a

 and 
[image: image12.wmf]2

a

 are the coefficients of thermal expansion (contraction) of the materials, 
[image: image13.wmf]t

D

 is the change in temperature,

                                         
[image: image14.wmf],

1

,

1

2

2

2

2

1

1

1

1

h

E

h

E

n

l

n

l

-

=

-

=

                                                           (3)

are the longitudinal axial compliances of the assembly components; 
[image: image15.wmf]1

h

and 
[image: image16.wmf]2

h

are the thicknesses of the components (in accordance with one of our assumptions, the thickness, 
[image: image17.wmf]2

h

, of the thicker component is significantly greater than the thickness, 
[image: image18.wmf]1

h

, of the thinner component); 
[image: image19.wmf]1

E

 and 
[image: image20.wmf]2

E

are the Young’s moduli of the component materials, 
[image: image21.wmf]1

n

 and 
[image: image22.wmf]2

n

are their Poisson’s ratios,

                 
[image: image23.wmf],

)

1

(

3

2

3

1

1

1

1

1

1

E

h

G

h

n

k

+

=

=

          
[image: image24.wmf]2

2

2

2

2

2

)

1

(

3

2

3

E

h

G

h

n

k

+

=

=

                               (4)

are the interfacial compliances of the assembly components [5, 6], 
[image: image25.wmf]1

G

and 
[image: image26.wmf]2

G

 are the shear moduli of the component materials, 
[image: image27.wmf])

(

x

t

is the interfacial shearing stress, 
                                               
[image: image28.wmf]ò

-

-

=

x

x

Y

l

d

x

T

*

*

)

(

)

(

t

x

x

t

                                                     (5)

are the thermally induced forces acting in the cross-sections of the assembly components, 
[image: image29.wmf]Y

t

 is the yield stress of the bonding material,  and 
[image: image30.wmf]*

l

 is the length of the plastic zone at the ends of the assembly. The length,
[image: image31.wmf]*

l

, can be defined as 
[image: image32.wmf]*

l

=
[image: image33.wmf]*

x

l

-

, where l is half the assembly length. The origin, 0, of the coordinate, x, is in the mid-cross-section of the assembly. 
The first terms in the right part of the expressions (2) are unrestricted (stress-free) displacements. The second terms determine the displacements due to the thermally induced forces,
[image: image34.wmf])

(

x

T

, that arise in the cross-sections of the assembly components, because of the thermal contraction mismatch of the dissimilar materials of the soldered components. These terms are defined based on the Hooke’s law assuming that all the points of the given cross-section have the same longitudinal displacements, i.e., the assembly cross-sections remain flat despite the change in the states of stress and strain.  The third terms in the right part of the equations (2) account for the inaccuracy of such an assumption and consider the fact that the interfacial displacements are somewhat larger than the displacements of the inner points of the cross-sections. The structure of these additional terms reflects an assumption that the displacements, which are responsible for the distortion in the planarity of the component’s cross-section, are proportional to the interfacial shearing stress acting in this cross-section. It is assumed also that these additional displacements are not affected by the stresses and strains in the adjacent cross-sections. 
While the structural analysis approach is used in this paper for the evaluation of stresses and displacements, the coefficients of proportionality (interfacial compliances) between the interfacial displacements and the interfacial shearing stresses are evaluated on the basis of the theory of elasticity solution [5]. This solution was obtained using Ribiere treatment of the problems for long-and-narrow strips subjected to the distributed shearing loads applied to one or to both of their long sides. 

The condition of the compatibility of the interfacial displacements, 
[image: image35.wmf])

(

1

x

u

  and  
[image: image36.wmf])

(

2

x

u

, can be written, considering the compliance

                                                       
[image: image37.wmf]0

0

0

0

0

0

)

1

(

2

E

h

G

h

n

k

+

=

=

                                              (6)

of the bonding layer [5], as follows:

                                                      
[image: image38.wmf])

(

)

(

)

(

0

2

1

x

x

u

x

u

t

k

-

=

                                                (7)

Here 
[image: image39.wmf]0

E

and 
[image: image40.wmf]0

n

 are the elastic constants of the bonding material, and 
[image: image41.wmf]0

h

 is the thickness of the bonding layer. 
Introducing the formulas (2) into the compatibility condition (7), we obtain the following basic integral equation for the shearing stress function,
[image: image42.wmf])

(

x

t

, in the elastic mid-portion of the assembly:

                                                
[image: image43.wmf]ò

D

D

=

-

x

tx

d

T

x

0

.

)

(

)

(

a

x

x

l

kt

                                           (8)

Here 
[image: image44.wmf]1

2

a

a

a

-

=

D

 is the thermal expansion (contraction) mismatch of the materials of the adherends,  
[image: image45.wmf]2

1

l

l

l

+

=

 is the total longitudinal axial compliance of the assembly, and 
[image: image46.wmf]2

1

0

k

k

k

k

+

+

=

 is the total longitudinal interfacial compliance of the assembly. It is noteworthy that, in the case of a thin and/or low modulus bonding layer, only the two soldered components (“adherends”) determine the axial compliance of the assembly. As to the interfacial compliance, both the soldered components (“adherends”) and the bonding layer (“adhesive”) contribute to the interfacial compliance: the role of a thin and low modulus bonding layer is typically comparable with the role of thick and high modulus bonded components (“adherends”), as one could see from the numerical example at the end of this paper.
Boundary Conditions

In the case, when plastic strains occur in the bonding material, the following conditions must be fulfilled at the boundary,
[image: image47.wmf]*

x

x

=

, between the “inner” (linearly elastic) and the “outer” (ideally plastic) zones:

                                                 
[image: image48.wmf],

)

(

*

Y

x

t

t

=

             
[image: image49.wmf]*

*

)

(

l

x

T

Y

t

-

=

                                 (9)

The first condition in (9) indicates that the shearing stress at the boundary between the elastic and the plastic zones must be equal to the yield stress. The second condition follows from the formula (5): the shearing stress,
[image: image50.wmf])

(

x

t

, is self-equilibrated, and therefore the integral in (5) is zero for 
[image: image51.wmf]*

x

x

=

. Physically, this condition is due to the fact that, since the interfacial shearing stress at the peripheral portions of the assembly is constant (is equal to the yield stress,
[image: image52.wmf]Y

t

), the force 
[image: image53.wmf])

(

x

T

changes linearly at these portions, from its value, 
[image: image54.wmf]*

l

Y

t

, at the boundary of the elastic and the plastic zones, to zero at the assembly ends. The sign “minus“ in front of the second boundary condition in (9) indicates that the force at the boundary should be compressive (negative) for the compressed component of the assembly. In the case of a purely elastic state of strain (
[image: image55.wmf])

0

*

=

l

, the following boundary condition should be fulfilled:

                                                           
[image: image56.wmf]ò

-

=

=

l

l

dx

x

l

T

0

)

(

)

(

t

                                              (10)

This condition reflects the fact that there are no external longitudinal forces acting at the end cross-sections of the assembly components.

Elasto-Plastic Solution

From (8) we find, by differentiation (with respect to the coordinate, x):

                                                     
[image: image57.wmf]t

x

T

x

D

D

=

-

¢

a

l

t

k

)

(

)

(

                                              (11)

The next differentiation, considering the relationship (5), yields:

                                                       
[image: image58.wmf]0

)

(

)

(

2

=

-

¢

¢

x

k

x

t

t

                                                   (12)

where
                                                               
[image: image59.wmf]k

l

=

k

                                                            (13)

is the parameter of the interfacial shearing stress. The equation (11) has the following solution in the elastic mid-portion of the assembly: 

                                                
[image: image60.wmf]*

sinh

sinh

)

(

kx

kx

x

Y

t

t

=

.                                                          (14)

It is clear that this solution satisfies the first condition in (9). Introducing the sought solution (14)  into the formula (5), we conclude that it satisfies also the second condition in (9). 

Introducing the solution (14) into the basic integral equation (8), we find that the relative length 
[image: image61.wmf]l

l

*

 of the plastic zone could be determined from the following transcendental equation:

                                     
[image: image62.wmf]ú

û

ù

ê

ë

é

÷

÷

ø

ö

ç

ç

è

æ

÷

ø

ö

ç

è

æ

-

-

=

¥

l

l

kl

kl

l

l

Y

*

max

*

1

coth

1

t

t

,                                            (15)

where

                                                             
[image: image63.wmf]l

a

t

t

k

D

D

=

¥

max

                                                   (16)

is the maximum elastic interfacial shearing stress at the end of an infinitely long assembly [5].

As evident from the equation (15), no plastic zones could possibly occur (
[image: image64.wmf])

0

*

£

l

, if the stress ratio 
[image: image65.wmf]Y

t

t

¥

max

of the maximum elastic shearing stress in an infinitely long assembly to the yield stress of the bonding material  is equal or smaller than the hyperbolic cotangent of the kl value:

                                                              
[image: image66.wmf]kl

Y

coth

max

£

¥

t

t

                                                    (17)

Indeed, for long (large l values) and/or stiff (large k values) assemblies, when coth kl could be considered equal to one, the condition (17) is equivalent to the requirement that the yield stress is simply larger than the maximum elastic interfacial shearing stress. In such a situation no plastic stresses could possibly occur. 

If the kl value is small, then the condition (17) results in the relationship:

                                                                  
[image: image67.wmf]l

t

Y

k

a

t

D

D

³

                                                  (18)

Thus, no plastic deformations could occur, if, in a short and/or compliant assembly, the condition (18) is fulfilled, i.e., if the yield stress 
[image: image68.wmf]Y

t

 is high, the assembly compliance 
[image: image69.wmf]k

in the denominator in the right part of the condition (18) is significant, the thermal strain 
[image: image70.wmf]t

D

D

a

 in the numerator is low, and the size, l,  of the assembly is small.

The equation (15), if solved for the lengths ratio in the parentheses, can be written also as

                              
[image: image71.wmf]1

1

ln

2

1

1

*

max

*

max

*

-

-

+

-

-

=

¥

¥

l

l

kl

l

l

kl

kl

l

l

Y

Y

t

t

t

t

                                                           (19)

If the yield stress 
[image: image72.wmf]Y

t

 is low and, for this reason, the stress ratio 
[image: image73.wmf]Y

t

t

¥

max

 is significantly larger than one, then, as evident from (19), 
[image: image74.wmf]l

l

=

*

, i.e., the entire interfacial zone is occupied by the plastic strains (stresses), regardless of weather the kl value is large or small.  If the stress ratio is significantly smaller than one, then the equation (19) yields:

                                                    
[image: image75.wmf]1

1

ln

2

1

1

*

*

*

+

-

-

=

l

l

kl

l

l

kl

kl

l

l

                                               (20)

As evident from this equation, plastic deformations might still take place, if the k value is large, despite the low l value. A possible numerical procedure for solving the equations (19) and (20) is shown in Appendix A.
Predicted Length of the Plastic Zone Based on an Elastic Solution

We proceed from the equation (12) and seek its elastic solution in the form similar to (14):

                                                 
[image: image76.wmf]kl

kx

C

x

sinh

sinh

)

(

=

t

                                                             (21)

Introducing (21) into the equation (12), we conclude that the following relationships must be fulfilled:

                                            
[image: image77.wmf]k

l

=

k

,    
[image: image78.wmf]kl

t

k

C

tanh

D

D

=

a

l

                                          (22)

The first formula in (22) is the same as the formula (13). This is because the formula (13) defines the parameter k of the elastic interfacial shearing stress. 

With the formulas (22), the solution (21) yields:

                         
[image: image79.wmf]kl

kx

kl

kx

kl

kl

kx

t

k

x

cosh

sinh

sinh

sinh

tanh

cosh

sinh

)

(

max

max

¥

¥

=

=

D

D

=

t

t

l

a

t

,                (23)

where 
[image: image80.wmf]¥

max

t

is the maximum shearing stress at the end of a very long and/or stiff assembly (
[image: image81.wmf])

¥

®

kl

. This stress is expressed by the formula (16). 
Putting 
[image: image82.wmf])

(

*

x

Y

t

t

=

in the formula (23), we obtain the following formula for the relative length 
[image: image83.wmf]l

x

l

l

*

*

1

-

=

 of the plastic zone:

                                                  
[image: image84.wmf](

)

[

]

2

*

1

1

ln

1

1

-

+

+

-

=

z

z

kl

l

l

,                                        (24)

where

                                                      
[image: image85.wmf]kl

z

Y

cosh

max

¥

=

t

t

                                                      (25)

For 
[image: image86.wmf]2

max

=

¥

Y

t

t

 and kl=2 the formula (24) yields 
[image: image87.wmf]3054

.

0

*

=

l

l

. Comparing this value with the value, 
[image: image88.wmf]4002

.

0

*

=

l

l

 obtained using the elasto-plastic solution, we conclude that in the case in question the prediction based on an elastic solution underestimates considerably (by about 24%) the length of the plastic zones. The underestimation is even greater (about 80%) in the numerical example carried out in the last section of this paper.
Peeling Stress

Basic Equation

The basic equation for the peeling stress, p(x), can be obtained using the following equation of equilibrium for the thinner (more flexible) component (#1) of the assembly treated as an elongated thin plate:

         
[image: image89.wmf]ú

ú

û

ù

ê

ê

ë

é

-

=

=

¢

¢

+

ò

ò

ò

-

-

-

x

x

Y

x

x

x

x

l

d

h

x

T

h

x

w

D

d

d

p

*

*

*

*

1

1

1

)

(

2

)

(

2

)

(

)

(

t

x

x

t

x

x

x

                                 (26)        where

                                                           
[image: image90.wmf])

1

(

12

2

1

3

1

1

1

n

-

=

h

E

D

                                                   (27)

is the flexural rigidity of the component, and w(x) is the deflection function of this component (with respect to the thicker component that, in accordance with our assumption, does not experience bending deformations). The equation (26) indicates that the “external” bending moment experienced by the component #1, and expressed by the right part in the equation (26) and the first term in the left part, should be equilibrated by the elastic bending moment, which is expressed by the second term in the left part of the equation (26). This term is proportional, for small deflections, to the second derivative (curvature) of the deflection function, w(x). 
In accordance with one of our assumptions, the peeling stress, p(x), can be evaluated as

                                                        
[image: image91.wmf])

(

)

(

x

Kw

x

p

=

,                                                     (28)

where K is the spring constant of the elastic foundation, provided by the bonding layer and, generally speaking, also by the assembly components themselves.
Excluding the deflection function, w(x), from the equations (26) and (28), we obtain the following integral equation for the peeling stress function,  p(x):

                                    
[image: image92.wmf])

(

2

)

(

)

(

1

1

*

*

x

T

h

x

p

K

D

d

d

p

x

x

x

x

=

¢

¢

+

ò

ò

-

-

x

x

x

                                          (29)

After differentiating this equation twice with respect to the coordinate x and considering the relationship (5), we obtain the following basic equation for the peeling stress function:

                                 
[image: image93.wmf]),

(

2

)

(

4

)

(

1

4

4

x

h

x

p

x

p

IV

t

b

b

¢

=

+

                                                   (30)

where

                                                                    
[image: image94.wmf]4

1

4

D

K

=

b

                                                  (31)

is the parameter of the peeling stress.

The equation (30) has the form of the equation of bending of a beam lying on a continuous elastic foundation (see, for instance, [12]) and loaded by a distributed load whose magnitude is proportional to the rate of changing in the interfacial shearing stress along the assembly. Since the shearing stress is constant outside the elastic region, the “peeling” stress is zero in this region. Note, that in the close proximity to the boundary between the elastic and plastic zones the peeling stress might change in a manner that violates its proportionality to the derivative of the shearing stress. This is due to the fact that the approximate solution (14) ignores the singularity at the boundary between the elastic and the inelastic zones, and therefore the behavior of the peeling stress in the proximity of this boundary might be different of what is described by the equation (30).
Boundary Conditions

The peeling stress should be self-equilibrated within the elastic region and therefore the following conditions of equilibrium with respect to the bending moments and the lateral forces should be fulfilled:

                                              
[image: image95.wmf]ò

ò

ò

-

-

-

=

=

*

*

*

*

*

0

)

(

,

0

)

(

x

x

x

x

x

x

d

p

d

d

p

x

x

x

x

x

                                     (32)

From (29) we find, by differentiation:

                                                
[image: image96.wmf])

(

2

)

(

)

(

1

1

*

x

h

x

p

K

D

d

p

x

x

t

x

x

=

¢

¢

¢

+

ò

-

                                      (33)

The relationships (29) and (33), with consideration of the conditions (32), result in the following boundary conditions for the peeling stress function, p(x):

      
[image: image97.wmf]Y

Y

l

h

D

Kl

h

x

p

t

b

t

*

1

4

1

*

1

2

4

)

(

*

-

=

-

=

¢

¢

, 
[image: image98.wmf]Y

Y

h

D

K

h

x

p

t

b

t

1

4

1

1

*

2

2

)

(

=

=

¢

¢

¢

                              (34)

The peeling stress in the zones of plastic shearing strains should be zero, as it follows from the equation (30): the shearing stress function is equal to the yield stress in these zones, and, hence, does not change along the assembly.

Solution to the Basic Equation

The equation (30) has the form of an equation of a beam lying on a continuous elastic foundation (see, for instance, [12]). We seek the solution to this equation in the form:

                                       
[image: image99.wmf]*

2

2

0

0

cosh

cosh

)

(

)

(

)

(

kx

kx

A

x

V

C

x

V

C

x

p

+

+

=

b

b

  ,                           (35)

where the functions 
[image: image100.wmf],

3

,

2

,

1

,

0

),

(

=

i

x

V

i

b

are expressed as follows:

                 
[image: image101.wmf])

cos

sinh

sin

(cosh

2

1

)

(

,

sin

sinh

)

(

,

cos

cosh

)

(

3

,

1

2

0

x

x

x

s

x

V

x

x

x

V

x

x

x

V

b

b

b

b

b

b

b

b

b

b

b

±

=

=

=

                                              (36)

These functions have the following properties 
                
[image: image102.wmf])

(

2

)

(

),

(

2

)

(

),

(

2

)

(

),

(

2

)

(

2

3

1

2

0

1

3

0

x

V

x

V

x

V

x

V

x

V

x

V

x

V

x

V

b

b

b

b

b

b

b

b

b

b

b

b

=

¢

=

¢

=

¢

-

=

¢

                                               (37)

which make their use of convenience. As evident from the expression (35), the peeling stress function, p(x), has its maximum value (zero derivative) at the origin, and is symmetric with respect to the mid-cross-section of the assembly. 
The first two terms in (35) provide the general solution to the homogeneous equation, which corresponds to the non-homogeneous equation (30), and the third term is the particular solution to this equation. Introducing this term into the equation (30), we obtain:

                                                      
[image: image103.wmf]*

4

1

coth

)

1

(

2

kx

kh

A

Y

h

t

+

=

   ,                                           (38)

where the ratio

                                                                  
[image: image104.wmf]2

b

h

k

=

                                                       (39)

characterizes the relative role of the interfacial shearing and peeling stresses.
Using the boundary conditions (34), we obtain the following algebraic equations for the constants 
[image: image105.wmf]0

C

 and 
[image: image106.wmf]2

C

 of integration: 

[image: image107.wmf]

 EMBED Equation.3  [image: image108.wmf]2

1

4

1

2

*

3

0

*

1

1

1

*

4

3

*

1

2

*

0

0

*

2

2

1

1

2

)

(

)

(

2

coth

1

2

2

)

(

)

(

F

h

h

C

x

V

C

x

V

F

h

kx

l

h

C

x

V

C

x

V

Y

Y

Y

Y

b

t

h

b

t

b

b

b

t

h

h

b

b

t

b

b

=

+

-

=

+

=

÷

÷

ø

ö

ç

ç

è

æ

+

+

=

-

                    (40) where

                                   
[image: image109.wmf]*

4

3

*

1

coth

1

2

kx

l

F

h

h

b

+

+

=

  ,          
[image: image110.wmf]4

2

1

1

h

+

-

=

F

.                    (41)                                                                                                   

The algebraic equations (40) have the following solutions:


[image: image111.wmf],

2

sin

2

sinh

)

(

)

(

2

*

*

1

*

3

2

*

0

1

0

x

x

F

x

V

F

x

V

h

C

Y

b

b

b

b

b

t

+

+

=

     
[image: image112.wmf]*

*

1

*

1

2

*

2

1

2

2

sin

2

sinh

)

(

)

(

2

x

x

F

x

V

F

x

V

h

C

Y

b

b

b

b

b

t

+

-

=

         (42)

This concludes the solution of the problem of finding the peeling stress function. Note that for long enough elastic zones the solution (35) can be simplified as follows:
  
[image: image113.wmf](

)

(

)

,

1

2

)]

(

cos[

)]

(

cos[

)]

(

sin[

2

)

(

4

1

*

2

*

*

1

)

(

1

*

h

t

b

b

b

b

t

b

+

+

+

ú

û

ù

ê

ë

é

-

+

-

-

-

=

-

-

kh

x

x

F

x

x

x

x

F

e

h

x

p

Y

x

x

Y

    (43)

and the hyperbolic cosine in the first formula in (41) can be put equal to one.

Numerical Example
Let a laser GaAs chip (Young’s Modulus E
[image: image114.wmf]1

=86GPa=8775.5kgf/mm
[image: image115.wmf]2

=12.5x10
[image: image116.wmf]6

psi; Shear Modulus G
[image: image117.wmf]1

=33GPa=3367.3kgf/mm
[image: image118.wmf]2

=4.788x10
[image: image119.wmf]6

psi; Coefficient of Thermal Expansion (CTE) α
[image: image120.wmf]1

=6.5x10
[image: image121.wmf]6

-

1/
[image: image122.wmf]0

C; Thickness h
[image: image123.wmf]1

=0.150mm; Width b
[image: image124.wmf]1

=0.4mm; Length 2l
[image: image125.wmf]1

= 2.4mm) be soldered, using 96.5%Ag3.5%Sn solder (Young’s Modulus E
[image: image126.wmf]a

=50.0GPa=1939.0kgf/mm
[image: image127.wmf]2

=2.7569x10
[image: image128.wmf]6

psi; Shear Modulus G
[image: image129.wmf]a

=19.0 GPa=737 kgf/mm
[image: image130.wmf]2

=1.048x10
[image: image131.wmf]6

psi; Estimated Yield Stress in Shear is 
[image: image132.wmf]0

.

15

=

Y

t

 MPa=1.5306 kgf/mm
[image: image133.wmf]2

=2176.0 psi;   Thickness h
[image: image134.wmf]a

=1mil=0.025mm), onto a Cu submount (substrate) (Young’s Modulus E
[image: image135.wmf]2

=110GPa=11224.5kgf/mm
[image: image136.wmf]2

=16.0x10
[image: image137.wmf]6

psi; Shear Modulus G
[image: image138.wmf]2

=46.0GPa=4693.9 kgf/mm
[image: image139.wmf]2

=6.675x10
[image: image140.wmf]6

psi; Coefficient of Thermal Expansion (CTE) α
[image: image141.wmf]2

=17.8x10
[image: image142.wmf]6

-

1/
[image: image143.wmf]0

C; Thickness h
[image: image144.wmf]2

=0.5mm; Width b
[image: image145.wmf]2

=4mm; Length 2l
[image: image146.wmf]2

= 4.8mm). In the computations that follow we assume 
[image: image147.wmf];

2

.

1

2

1

mm

l

l

l

=

=

=

 and, for the sake of simplicity and for illustrative purposes, we assume also that the chip and the substrate have the same width. The soldering temperature is about 158
[image: image148.wmf]0

C, so that the change in temperature can be assumed to be 
[image: image149.wmf]=

D

t

125
[image: image150.wmf]0

C. 
The Poisson’s ratios of the bonded components and the bonding material are 
[image: image151.wmf]2

.

0

1

2

,

32

.

0

1

2

,

3

.

0

1

2

2

2

2

1

1

1

=

-

=

=

-

=

=

-

=

G

E

G

E

G

E

a

a

a

n

n

n

. Then the formulas (3), (4) and (6) result in the following axial and interfacial compliances of the materials: 

[image: image152.wmf]kg

mm

x

h

E

kg

mm

x

h

E

/

10

4254

.

1

1

;

/

10

3178

.

5

1

4

2

2

2

2

4

1

1

1

1

-

-

=

-

=

=

-

=

n

l

n

l

;        
[image: image153.wmf]kg

mm

x

/

10

7432

.

6

4

2

1

-

=

+

=

l

l

l



[image: image154.wmf],

/

10

3551

.

0

)

1

(

3

2

3

,

/

10

1485

.

0

)

1

(

3

2

3

3

4

2

2

2

2

2

2

3

4

1

1

1

1

1

1

kg

mm

x

E

h

G

h

kg

mm

x

E

h

G

h

-

-

=

+

=

=

=

+

=

=

n

k

n

k



[image: image155.wmf]3321

.

0

)

1

(

2

0

0

0

0

0

0

=

+

=

=

E

h

G

h

n

k

x
[image: image156.wmf],

/

10

3

4

kg

mm

-

     
[image: image157.wmf]x

8357

.

0

2

1

0

=

+

+

=

k

k

k

k



 EMBED Equation.3  [image: image158.wmf]kg

mm

/

10

3

4

-


The parameter k of the interfacial shearing stress, in accordance with the formula (13), is as follows:  


[image: image159.wmf]1

8406

.

2

-

=

=

mm

k

k

l


Hence, the parameter kl is kl=3.4087. From (16) we find the following  value of the maximum elastic interfacial shearing stress, if the bonding material behaves elastically under any level of loading:


[image: image160.wmf]2

max

/

9502

.

5

mm

kg

t

k

=

D

D

=

¥

l

a

t


The ratio 
[image: image161.wmf]¥

max

t

/
[image: image162.wmf]Y

t

 is 3.8875, so that the equation (19) yields: 
[image: image163.wmf],

7334

.

0

*

=

l

l

 i.e., about 26.6% of the interface’s length experiences elastic deformations. The flexural rigidity of the thinner component #1 can be found by the formula (27): 

[image: image164.wmf])

1

(

12

2

1

3

1

1

1

n

-

=

h

E

D

=2.7122 kg x mm
In an approximate analysis we assume that the spring constant of the elastic foundation can be put equal to the Young’s modulus of the bonding material, so that K=E
[image: image165.wmf]0

=1939kgf/mm
[image: image166.wmf]2

. The coordinate
[image: image167.wmf]*

x

 of the plastic zone is
[image: image168.wmf]mm

l

l

x

3199

.

0

*

*

=

-

=

, and therefore 
[image: image169.wmf]*

kx

=0.9088, and coth
[image: image170.wmf]*

kx

=1.3878.  Hence, in the case in question, the elastic zone cannot be assumed to be infinitely long. The formulas (31), (38) and (39) yield:


[image: image171.wmf]1

4

1

6564

.

3

4

-

=

=

mm

D

K

b

;  
[image: image172.wmf]1697

.

1

*

=

x

b

; 
[image: image173.wmf]54934

.

0

2

=

=

b

h

k

;
[image: image174.wmf]2

*

4

1

/

7185

.

0

coth

)

1

(

2

mm

kg

kx

kh

A

Y

=

+

=

h

t

;
The functions 
[image: image175.wmf])

(

*

x

V

i

b

, which are expressed by the formulas (36), have the following values:


[image: image176.wmf];

7458

.

0

)

1697

.

1

(

)

(

;

3350

.

1

)

1697

.

1

(

)

(

;

5537

.

1

)

1697

.

1

(

)

(

;

6917

.

0

)

1697

.

1

(

)

(

3

*

3

2

*

2

1

*

1

0

*

0

=

=

=

=

=

=

=

=

V

x

V

V

x

V

V

x

V

V

x

V

b

b

b

b


The formulas (41) and (42) yield: 
[image: image177.wmf]2

2

2

0

2

1

/

4822

.

2

;

/

8401

.

0

;

9165

.

0

,

7651

.

4

mm

kg

C

mm

kg

C

F

F

-

=

=

-

=

=


Then the peeling stress function expressed by the solution (35) is as follows:


[image: image178.wmf])

8406

.

2

cosh(

4988

.

0

)

6564

.

3

(

4822

.

2

)

6564

.

3

(

8401

.

0

)

(

2

0

x

x

V

x

V

x

p

+

-

=


The calculated interfacial shearing and the peeling stresses are plotted in Fig.2. As evident from this plot, one cannot simply truncate the diagram for the shearing stress, obtained on the basis of an elastic solution, to evaluate the length of the plastic zone. Such an approach will result in a substantial, by about 80%, underestimation of the length of the plastic zone. Clearly, the elastic approach cannot be used to assess the peeling stress either.
Conclusions

The following conclusions can be drawn from the performed analysis:

· A simple and easy-to-use transcendental equation has been obtained for the evaluation of the length of the plastic (inelastic) zone in a low-yield-stress bonding layer of a bi-material assembly subjected to the change in temperature

· The obtained solutions can be used for the analysis and design of the bonded assemblies with a bonding material that has a low yield point. . The obtained solutions can be useful, particularly, when developing figures-of-merit (design criteria) for the assemblies of the type in question.  
References

1. S.Timoshenko, “Analysis of Bi-Metal Thermostats”, Journal of the Optical Society of America, vol.11, 1925.

2. B.J.Aleck, “Thermal Stresses in a Rectangular Plate Clamped Along an Edge”, ASME Journal of Applied Mechanics, vol.16, 1949.

3. W.T. Chen and C.W.Nelson, “Thermal Stresses in Bonded Joints”, IBM Journal, Research and Development, vol.23, No.2, 1979.

4. F.-V. Chang,  “Thermal Contact Stresses of Bi-Metal Strip Thermostat”, Applied Mathematics and Mechanics, vol.4, No.3, Tsing-hua Univ., Beijing, China, 1983.

5. E. Suhir, “Stresses in Bi-Metal Thermostats”, ASME Journal of Applied Mechanics, vol. 53, No. 3, Sept. 1986.

6. E. Suhir, “Interfacial Stresses in Bi-Metal Thermostats”, ASME Journal of Applied Mechanics, vol. 56, No. 3, September 1989.

7. E. Suhir, “Calculated Thermally Induced Stresses in Adhesively Bonded and Soldered Assemblies”,  Proc. of the Int. Symp. on Microelectronics, ISHM, 1986, Atlanta, Georgia, Oct. 1986. 

8. R. Zeyfang, “Stresses and Strains in a Plate Bonded to a Substrate: Semiconductor Devices”, Solid State Electronics, vol.14, 1971

9. J.W. Eischen, C.Chung and J.H.Kim, “Realistic Modeling of the Edge Effect Stresses in Bimaterial Elements”, ASME Journal of Electronic Packaging, vol.112, No.1, 1990.

10. A.Y.Kuo, “Thermal Stress at the Edge of a Bi-Metallic Thermostat”, ASME Journal of Applied Mechanics, vol.57, 1990.

11. S. E. Yamada, “A Bonded Joint Analysis for Surface Mount Components”, ASME Journal of Electronic Packaging, vol.114, No.1, 1992

12. E. Suhir, “Structural Analysis in Microelectronic and Fiber Optic Systems” , Van Nostrand Reinhold, New York, 1991.

13. J.C. Glaser, “Thermal Stresses in Compliantly Joined Materials”, ASME Journal of Electronic Packaging, vol.112, No.1, 1990.

14. E. Suhir, “Die Attachment Design and Its Influence on the Thermally Induced Stresses in the Die and the Attachment”, Proc. of the 37th Elect. Comp. Conf., IEEE, Boston, Mass., May 1987.

15. V. Mishkevich and E. Suhir, “Simplified Approach to the Evaluation of Thermally Induced Stresses in Bi-Material Structures”, in E. Suhir, ed., “Structural Analysis in Microelectronics and Fiber Optics”, ASME Press, 1993.

16. E. Suhir, "Analysis of Interfacial Thermal Stresses in a Tri-Material Assembly", Journal of Applied Physics, vol.89, No.7, 2001

Appendix   A

Transcendental Equation for the Relative Length of the Plastic Zone
The transcendental equations (15) and (19) of the main text can be solved numerically. Let, for instance, the stress ratio be equal to 
[image: image179.wmf]Y

t

t

¥

max

=2, and the parameter kl is also equal to kl=2. Then the equation (15) yields:

                                                         
[image: image180.wmf]ú

û

ù

ê

ë

é

÷

ø

ö

ç

è

æ

-

-

=

l

l

l

l

*

*

1

2

coth

2

1

1

                                   (A-1)

This equation has the following solution: 
[image: image181.wmf].

4002

.

0

*

=

l

l

 This result could be obtained by simply assuming different length ratios, plotting the function in the right part of the equation (A-1) and accepting, as a solution, the length ratio, which is equal to the computed value of this function in the left part of the equation. The same result can be obtained from the equation (19).

Another approach is to employ a rapidly converging iterative numerical procedure. Such a procedure can be based on the well-known Newton’s formula

                                                     
[image: image182.wmf])

(

)

(

1

n

n

n

n

x

f

x

f

x

x

¢

-

=

+

                                                   (A-2)

for solving a transcendental equation  f(x)=0. 

The formula of the (A-2) type can be obtained from the equation (15) as follows: 

                                    
[image: image183.wmf](

)

(

)

1

2

1

2

*

*

*

max

*

1

*

-

÷

ø

ö

ç

è

æ

-

÷

÷

ø

ö

ç

ç

è

æ

-

+

÷

ø

ö

ç

è

æ

=

÷

ø

ö

ç

è

æ

¥

+

n

n

n

Y

n

n

z

l

l

z

kl

l

l

l

l

t

t

                            (A-3) 

where

                                                        
[image: image184.wmf]ú

û

ù

ê

ë

é

÷

ø

ö

ç

è

æ

-

=

l

l

kl

z

*

*

1

coth

                                            (A-4)

For 
[image: image185.wmf]Y

t

t

¥

max

=2 and kl=2, assuming, in the zero approximation,  
[image: image186.wmf],

5

.

0

0

*

=

÷

ø

ö

ç

è

æ

l

l

 we obtain: 
[image: image187.wmf],

4361

.

0

1

*

=

÷

ø

ö

ç

è

æ

l

l



 EMBED Equation.3  [image: image188.wmf],

4101

.

0

2

*

=

÷

ø

ö

ç

è

æ

l

l



 EMBED Equation.3  [image: image189.wmf]4026

.

0

3

*

=

÷

ø

ö

ç

è

æ

l

l

, 
[image: image190.wmf]4007

.

0

4

*

=

÷

ø

ö

ç

è

æ

l

l

, 
[image: image191.wmf]4003

.

0

5

*

=

÷

ø

ö

ç

è

æ

l

l

,

[image: image192.wmf]4002

.

0

6

*

=

÷

ø

ö

ç

è

æ

l

l


No iterations are necessary for sufficiently long and stiff assemblies, characterized by large kl values, since the hyperbolic cotangent will be equal to “one” for any (but large enough) value of the argument. Indeed, let kl be equal to kl=10. Then, assuming that the 
[image: image193.wmf]l

l

*

  ratio is significantly smaller than one, we have 
[image: image194.wmf]1

*

»

z

 and the equation (A-3) yields:


[image: image195.wmf](

)

2

.

0

1

2

10

2

1

2

max

1

*

=

-

=

÷

÷

ø

ö

ç

ç

è

æ

-

=

÷

ø

ö

ç

è

æ

¥

+

Y

n

kl

l

l

t

t



[image: image196]
Fig.1. Bi-Material Assembly with a Thin and Low-Yield-Stress Bonding Layer
[image: image197.emf]-3

-2

-1

0

1

2

3

4

5

6

0 0.1 0.2 0.3 0.4 0.5 0.6 0.7 0.8 0.9 1 1.1 1.2

Distance from the mid-cross-section of the assembly, mm

Interficial Stresses (kg/mm2)

Elastic Zone Plastic Zone



y



Elastic shearing stress

Elasto-Plastic

Shearing stress

Peeling stress

Mid-cross-section of the 

assembly

Yield stress


Fig. 2.  Calculated Interfacial Stresses
E2,v2,α2





E1,v1,α1





h2





E0,v0





l





l





GaAs Chip:


Component #1





Bonding layer:


 “Zero” Component


     





Cu Submount:


Component #2





x





h0





h1












































PAGE  
16

_1189786217.unknown

_1201949757.unknown

_1207167996.unknown

_1218570880.unknown

_1222933619.unknown

_1223118338.unknown

_1223127107.unknown

_1223127171.unknown

_1223192321.unknown

_1223127147.unknown

_1223127065.unknown

_1222889487.unknown

_1222890204.unknown

_1222892608.unknown

_1222894184.unknown

_1222890296.unknown

_1222889500.unknown

_1222889338.unknown

_1222889415.unknown

_1207395315.unknown

_1218569674.unknown

_1218570879.unknown

_1218569609.unknown

_1218569644.unknown

_1218569562.unknown

_1207321816.unknown

_1207321927.unknown

_1207323042.unknown

_1207168013.unknown

_1207233061.unknown

_1201953154.unknown

_1207152332.unknown

_1207152399.unknown

_1207153541.unknown

_1207163111.unknown

_1207152379.unknown

_1207152261.unknown

_1201955508.unknown

_1201953893.unknown

_1201953943.unknown

_1201950074.unknown

_1190161059.unknown

_1197805359.unknown

_1197805855.unknown

_1197806126.unknown

_1197817546.unknown

_1201892249.unknown

_1201898849.unknown

_1201948376.unknown

_1201948854.unknown

_1201949095.unknown

_1201949353.unknown

_1201949057.unknown

_1201948716.unknown

_1201899006.unknown

_1201929296.unknown

_1201898945.unknown

_1201894646.unknown

_1201898350.unknown

_1201894624.unknown

_1197817764.unknown

_1197817107.unknown

_1197817354.unknown

_1197817391.unknown

_1197807593.unknown

_1197815293.unknown

_1197815390.unknown

_1197816898.unknown

_1197817062.unknown

_1197815656.unknown

_1197815345.unknown

_1197814867.unknown

_1197815210.unknown

_1197807582.unknown

_1197805844.unknown

_1190403228.unknown

_1197801524.unknown

_1197802169.unknown

_1197802638.unknown

_1197804853.unknown

_1197804997.unknown

_1197804199.unknown

_1197802445.unknown

_1197802022.unknown

_1197802153.unknown

_1197801996.unknown

_1190919397.unknown

_1197800005.unknown

_1197800235.unknown

_1197800294.unknown

_1190985761.unknown

_1197799959.unknown

_1190403269.unknown

_1190283988.unknown

_1190285300.unknown

_1190402434.unknown

_1190403145.unknown

_1190284109.unknown

_1190161514.unknown

_1189819258.unknown

_1190036646.unknown

_1190160224.unknown

_1190161032.unknown

_1190037539.unknown

_1189950687.unknown

_1189819445.unknown

_1189820073.unknown

_1189817001.unknown

_1189818778.unknown

_1189818935.unknown

_1189818121.unknown

_1189787617.unknown

_1189816979.unknown

_1189786756.unknown

_1189787247.unknown

_1189787327.unknown

_1189786663.unknown

_1189737851.unknown

_1189740085.unknown

_1189740324.unknown

_1189740601.unknown

_1189743066.unknown

_1189745162.unknown

_1189767996.unknown

_1189768368.unknown

_1189768882.unknown

_1189767270.unknown

_1189744281.unknown

_1189745101.unknown

_1189743569.unknown

_1189741998.unknown

_1189742663.unknown

_1189740960.unknown

_1189740386.unknown

_1189740129.unknown

_1189738930.unknown

_1189739288.unknown

_1189739663.unknown

_1189739736.unknown

_1189739802.unknown

_1189739359.unknown

_1189739131.unknown

_1189739255.unknown

_1189738985.unknown

_1189738300.unknown

_1189738880.unknown

_1189737896.unknown

_1189737049.unknown

_1189737346.unknown

_1189737416.unknown

_1189737777.unknown

_1189737388.unknown

_1189737277.unknown

_1189737318.unknown

_1189737244.unknown

_1189736853.unknown

_1189736954.unknown

_1189737008.unknown

_1189736910.unknown

_1189733057.unknown

_1189736807.unknown

_1189736214.unknown

_1189736307.unknown

_1189733172.unknown

_1189732993.unknown

